Crack in pool
shell at skimmer elevation.

Cracks in pool beam.

Photograph 31

Cracks in pool beam and in pool shell at skimmer elevation.

Locations of trip hazards.

Settlement of pool deck.

Photograph 32

Settlement in concrete pool deck. Settlement has caused trip hazards.

Cracks in pool deck

Photograph 33 Cracks in concrete pool deck.

Photograph 34

Varsity Club / Administration Building

Column cracking / spall

Photograph 35 Localized column cracking / spall.

Photograph 36

Cracking of floor finish, cause unknown and requires further evaluation.

Photograph 37

Water damage to floor finish due to window leaks.

Photograph 38

Roof tile damage. Undulations in roof plane. Visual roof damage is approximately over encountered roof leak.

Soffit and fascia framing damage.

Roof gutter system joint.

Photograph 39

Water damage to roof truss, fascia framing, and soffit framing. Damage occurred at internal roof drain system joint.

Photograph 40 Pro-Shop Building

Photograph 41

Delaminated stucco finish on site / garden wall.

Photograph 42 Cracked / failing site wall.

Settlement of concrete apron slab.

Photograph 43

Settlement of concrete apron slab producing trip hazards.

Photograph 44

Exterior concrete apron slab on fill was placed higher than the interior slab and storefront window system.
Any wind driven rain that reaches storefront can not drain off properly. Water must drain into the fill material or into the interior of the building.

Photograph 45 Cart Barn Building

Photograph 46 Damaged aluminum wall panels.

Photograph 47

Inadequate car porch roof beam splice. Beam should span from post to post. Split with inadequate detailing makes beam susceptible to failure

Water damage to roof sheathing, roof ribbon board and end of roof truss.

Photograph 48 Evidence of roof leak.

Photograph 49 Locker Room Building

Photograph 50 Tile wall finish failure.

Photograph 51

Roof fascia stucco failures. Wind driven rain can penetrate failed finish into interior.

Cracking in exterior wall.

Photograph 52

Stair step cracking in masonry wall due to either settlement or unstrained thermal movement.

Photograph 53

Build up of organic debris on top of room.

Photograph 54

Separation in roof parapet wall roof flashing. Condition leaves integrity of roofing in question.

Approximate ½” gap.

Photograph 55

Separation in roof parapet roof flashing.

Photograph 56

Exposed, non-roofed abandoned mechanical roof rack. Water has direct path into and possible under roofing material. Condition will reduce service life of roof.

Photograph 57

Tennis & Fitness Center Building

Differential settlement in concrete slab. Trip hazard.

Photograph 58

Settlement of the concrete apron slab and sidewalk. Settlement has reached the degree which produced trip hazard.